EXPERIMENTAL STUDY ON FLEXURAL BEHAVIOUR OF POLYPROPYLENE FIBRE REINFORCED CONCRETE T-BEAMS

Chitra.S1

1 PG Student

Department of Civil Engineering

1Sree Sastha Institute of Engineering Technology, Chembarambakkam,

Chennai,TamilNadu

er.chitra001@gmail.com1

Abstract: Fibre  reinforced  concrete  is  one  of  the  effective  ways  of  improving  the  performance  of  concrete. The  use  of  polypropylene  fibers  in  concrete  is  to  reduce  the  crack  width, crack  propagation, plastic  shrinkage  cracks  and  settlement  cracking  during  the  early  age  of  the  concrete. An  experimental  study  on  flexural  behavior  of  polypropylene  fibre  reinforced  concrete          T-beams  is  to  be  conducted. Three  number  of  T-beams  using  M20  grade  concrete  by  adding  polypropylene  fibre  as  control  specimen(0%), 0.5%, 1%  by  weight  of  cement. The  polypropylene  fibers  will  be  distributed  randomly  throughout  the  concrete  at  the  time  of  mixing. Flexure  behavior test  is  to  be  conducted  by  two  point  loading  arrangement. The  experimental  result  shows  that  when  increasing  the  fibre  percent  it  increases  the  strength  of  the T-Beam.

Key Words: Fiber, Crack, polypropylene

I.INTRODUCTION

Concrete  and  steel  were  always  considered as  the  most  important  commonly  used   structural  materials. The  development  of  new  high  performance  composite  materials  that  are  stronger  and  more  durable  in  conventional  materials  (e.g., Portland  cement  concrete,  steel,  wood  and  masonry)  is  important  to  the  construction  industry.

II.POLYPROPYLENE FIBRE

Polypropylene  fibers  are  tough  but  have  low  tensile  strength  and  modulus  of  elasticity. Polypropylene  fibre  concrete  is  versatile  and  can  be  used  in  most  applications. Thousands  of  individual  fibres  are  then  evenly  dispersed  through  out  the  concrete  during  the  mixing  process  creating  a  matrix-like  structure.

III. TESTING OF MATERIALS

Table 1: Specific Gravity of Materials

| S.NO. | MATERIALS | SPECIFIC GRAVITY |
| --- | --- | --- |
| 1. | Cement | 3.15 |
| 2. | Fine Aggregate | 2.61 |
| 3. | Coarse Aggregate | 2.62 |

IV. MIX DESIGN

Table 2: Mix proportion values

| S.NO | MATERIALS | Kg/m3 |
| --- | --- | --- |
| 1 | Cement | 389 |
| 2 | Fine Aggregate | 550 |
| 3 | Coarse Aggregate | 1206 |
| 4 | Water | 195 |

V.EXPERIMENTAL PROGRAM

The test program consist of three T-beams. Three  number  of  T-Beams  using  M20  grade concrete  by  adding  polypropylene  fibre  as  control  specimen(0%), 0.5%, 1%   by  weight  of  cement. The  polypropylene  fibers  will  be  distributed  randomly  throughout  the  concrete  at  the  time  of  mixing. Flexural  behavior  test  is  to  be  conducted  by  two  point  loading  arrangement.

Fig. 1: Loading arrangement

VI. T- BEAM DESIGN

Fig. 2: T- beam design

VII.RESULTS AND DISCUSSIONS

7.1 Flexural Test

| S.No | Load in KN | Deflection in mm |  |  |
| --- | --- | --- | --- | --- |
|  |  | Control Specimen (0%) | 0.5%fibre | 1%fibre |
| 1 | 0 | 0 | 0 | 0 |
| 2 | 5 | 0.20 | 0.18 | 0.13 |
| 3 | 7.5 | 0.32 | 0.24 | 0.21 |
| 4 | 10 | 0.41 | 0.35 | 0.29 |
| 5 | 15 | 0.53 | 0.44 | 0.37 |
| 6 | 17.5 | 0.67 | 0.55 | 0.43 |
| 7 | 20 | 0.76 | 0.64 | 0.52 |
| 8 | 25 | 0.85 | 0.76 | 0.64 |
| 9 | 27.5 | 0.96 | 0.83 | 0.75 |
| 10 | 30 | 1.10 | 0.95 | 0.84 |
| 11 | 35 | 1.25 | 1.12 | 1.06 |
| 12 | 37.5 | 1.36 | 1.27 | 1.15 |
| 13 | 40 | 1.47 | 1.35 | 1.24 |
| 14 | 45 | 1.56 | 1.44 | 1.37 |
| 15 | 47.5 | 1.67 | 1.55 | 1.42 |
| 16 | 50 | 1.75 | 1.64 | 1.53 |
| 17 | 55 | 1.82 | 1.78 | 1.65 |

Flexure Test results for T-Beam Control Specimen (0%), 0.5%fibre, 1%fibre at One-Third left

Deflection in mm

Fig.3: Load   Deflection Curve for  Control  Specimen(0%)  at  One-Third  Left

Load in KN

Deflection in mm

Fig.4 Load Deflection Curve for  0.5% Polypropylene Fibre at One-Third  Left

Deflection in mm

Fig.5: Load  Deflection Curve for 1% Polypropylene Fibre at One-Third Left

Table 2:  Flexure Test results for T-Beam control specimen (0%), 0.5%fibre, 1%fibre at Middle.

| S.No | Load in KN | Deflection in mm |  |  |
| --- | --- | --- | --- | --- |
|  |  | Control Specimen (0%) | 0.5%fibre | 1%fibre |
| 1 | 0 | 0 | 0 | 0 |
| 2 | 5 | 0.37 | 0.21 | 0.10 |
| 3 | 7.5 | 0.42 | 0.38 | 0.27 |
| 4 | 10 | 0.54 | 0.47 | 0.38 |
| 5 | 15 | 0.60 | 0.51 | 0.46 |
| 6 | 17.5 | 0.71 | 0.63 | 0.50 |
| 7 | 20 | 0.82 | 0.70 | 0.64 |
| 8 | 25 | 0.93 | 0.82 | 0.71 |
| 9 | 27.5 | 1.02 | 0.91 | 0.80 |
| 10 | 30 | 1.14 | 1.06 | 1.01 |
| 11 | 35 | 1.31 | 1.27 | 1.13 |
| 12 | 37.5 | 1.42 | 1.34 | 1.21 |
| 13 | 40 | 1.53 | 1.41 | 1.30 |
| 14 | 45 | 1.62 | 1.50 | 1.41 |
| 15 | 47.5 | 1.73 | 1.61 | 1.53 |
| 16 | 50 | 1.84 | 1.70 | 1.62 |
| 17 | 55 | 1.93 | 1.82 | 1.78 |

Deflection in mm

Fig.6: Load Deflection Curve for Control Specimen (0%) at Middle

Deflection in mm

Fig.7: Load Deflection Curve for 0.5% Polypropylene Fibre at Middle

Deflection in mm

Fig.8: Load Deflection Curve  for  1% Polypropylene Fibre at Middle

Table 3:Flexure  Test  results  for  T-Beam  Control  Specimen(0%), 0.5%fibre, 1%fibre  at  One-Third  right.

| S.No | Load in KN | Deflection in mm |  |  |
| --- | --- | --- | --- | --- |
|  |  | Control Specimen(0%) | 0.5%fibre | 1%fibre |
| 1 | 0 | 0 | 0 | 0 |
| 2 | 5 | 0.20 | 0.17 | 0.15 |
| 3 | 7.5 | 0.34 | 0.26 | 0.23 |
| 4 | 10 | 0.42 | 0.38 | 0.30 |
| 5 | 15 | 0.55 | 0.46 | 0.38 |
| 6 | 17.5 | 0.69 | 0.58 | 0.46 |
| 7 | 20 | 0.78 | 0.67 | 0.55 |
| 8 | 25 | 0.87 | 0.79 | 0.68 |
| 9 | 27.5 | 0.99 | 0.86 | 0.77 |
| 10 | 30 | 1.12 | 0.97 | 0.88 |
| 11 | 35 | 1.29 | 1.15 | 1.09 |
| 12 | 37.5 | 1.38 | 1.29 | 1.17 |
| 13 | 40 | 1.49 | 1.37 | 1.26 |
| 14 | 45 | 1.58 | 1.46 | 1.39 |
| 15 | 47.5 | 1.69 | 1.57 | 1.45 |
| 16 | 50 | 1.77 | 1.68 | 1.56 |
| 17 | 55 | 1.84 | 1.79 | 1.67 |

Deflection in mm

Fig.9: Load Deflection Curve for Control Specimen(0%) at One-Third Right

Deflection in mm

Fig.10: Load Deflection Curve for 0.5%Polypropylene Fibre at One-Third Right

Deflection in mm

Fig.11: Load Deflection Curve  for  1%Polypropylene Fibre at One-Third Right

7.2 COMPRESSIVE STRENGTH TEST

Table 3.  Test Result for Cube

| % of fibre | Failure load in tonnes | Compressive Strength N/mm2 |
| --- | --- | --- |
| 0% | 22.97 | 10.01 |
| 0.5% | 27.54 | 12.02 |
| 1% | 36.83 | 16.06 |

Percent of Fibre

Fig.12:  Percent of Fibre and Compressive Strength for the Cube

7.3 SPLIT TENSILE STRENGTH TEST

Table 4: Test Result for Cylinder

| % of fibre | Failure load in tonnes | Tensile Strength N/mm2 |
| --- | --- | --- |
| 0% | 17.98 | 1.248 |
| 0.5% | 19.86 | 1.378 |
| 1% | 21.69 | 1.505 |

Percent of Fibre

Fig.13: Percent  of Fibre and  Tensile Strength for the Cylinder

7.4 Failure  of  all  T-Beams

7.5 DISCUSSIONS

In  experimental  results  the  middle  deflection 500mm  for  T-beam  the  control specimen(0%) is 1.93mm  it  increases  when  comparing  the  One-Third left 250mm  the  deflection  value  is  1.82mm  and  the  One-Third  right 750mm  the  deflection  value  is  1.84mm.In  experimental  results  the  middle  deflection 500mm  for  T-beam  0.5% fibre is 1.90mm  it  increases  when  comparing  the  One-Third left 250mm  the  deflection  value  is  1.85mm  and  the  One-Third  right 750mm  the  deflection  value  is  1.87mm.In  experimental  results  the  middle  deflection 500mm  for  T-beam  1% fibre is 2.11mm  it  increases  when  comparing  the  One-Third left 250mm  the  deflection  value  is  2.07mm  and  the  One-Third  right 750mm  the  deflection  value  is  2.09mm.When  increasing  the  fibre  percent(0.5%,1%)it  increases  the  strength  of  the  T-Beam.The  failure  load  for  controlspecimen(0%), 0.5%fibre, 1% fibre  is  22.97tonnes, 27.54tonnes, 36.83tonnes for  compressive  strength  of  cube10.01N/mm2,12.02N/mm2,16.06N/mm2increases  when  increasing  the  fibre  percent(0.5%,1%)  in  concrete. The  failure  load  for  control specimen(0%), 0.5%fibre, 1% fibre  is  17.98tonnes, 19.86tonnes, 21.69tonnes  for  tensile  strength of the  cylinder is 1.248N/mm2,1.378N/mm2,1.505N/mm2 increases when  increasing  the  fibre  percent(0.5%,1%)  in  concrete.

VIII.CONCLUSION

From  the  experimental  study  it  is  observed  that  the  ultimate  load  carrying  capacity  for  T-Beam  control  specimen(0%)  is  55KN.    The  Ultimate  load  carrying  capacity  for  T-Beam  0.5% Polypropylene  fibreis  57.5KN  when  comparing  to  the  control  specimen(0%)  it  increases  2.5KN. The  Ultimate  load  carrying  capacity  for  T-Beam  1%   fibreis  60KN  when  comparing  to  the  control  specimen(0%)   it  increases  5KN  and  0.5% fibre  it  increases  2.5KN.The  failure  load  in  compressive  strength  for  control  specimen(0%)  is  10.01N/mm2. The  failure  load  in  compressive  strength  for  0.5% fibre  is  12.02N/mm2  when  comparing  to  the  0%  it  increases  2N/mm2.The  failure  load  in  compressive  strength  for  1% fibre  is  16.06N/mm2 when  comparing  to  the  0%  it  increases  6N/mm2  and  0.5% fibre  it  increases  4N/mm2.The  failure  load  in  tensile  strength  for  control  specimen(0%)  is  1.248N/mm2. The  failure  load  in  tensile  strength  for  0.5% fibre  is  1.378N/mm2  when  comparing  to  the  0%  it  increases  0.13N/mm2. The  failure  load  in  tensile  strength  for  1% fibre  is  1.505N/mm2 when  comparing  to  the  0%  it  increases  0.26N/mm2  and  0.5% fibre  it  increases  0.13N/mm2. The  load  carrying  capacity  for  T-Beam  is increased  by  the use  of  percentage  of  fibres.

IX.REFERENCES

1)SinaphM.	Namboorimadathil, J.GustavoTumialan, Antonio Nanni (1991),‘Behaviour  of  RC T-Beams  Strengthened  in  the  Negative  Moment  Region  With  Carbon  Fibre  Reinforced  Polymer  (CFRP)  Laminates’,Journal  of Structural  Engineering,volume:117, Issue No:11, pp.1-92.

2) M.S.Ellison  and  E.Corona(1998),‘An  Experimental  Investigation  of  T-Beam  Stability  Under  Bending’, Journal  on  Experimental  Mechanics, Volume:38, Issue No:1, pp.42-47.

3) Fang  Zhi  and  Yang  Jian (2003),‘Behaviour  of  concrete  T-Beams  Prestressed  With  Partially  Bonded  CFRP  Tendons’, ACI  Structural  Journal,  Volume:93, Issue No:1,pp.1-6.

4) Christophe  Deniaud  and  J.J.Roger  Cheng (2003), ‘Reinforced  Concrete  T-Beams  Strengthened  in  Shear  With  Fiber  Reinforced  Polymer  Sheets’, Journal  of  Composites  for  Construction ,Volume:7, Issue No:4, pp.302-310.

5)PitiSukontasukkul (2004), ‘Toughness  Evaluation  of  Steel  and  Polypropylene  Fibre  Reinforced  Concrete  Beams  under  Bending’, Journal  of  Science  and  Technology, Volume:9, Issue No:3, pp.35-41.

6)Kyle H.Larson, Robert J. Peterman  and  Hayder A. Rasheed (2005),‘Strength- Fatigue  Behaviour  of  Fibre  Reinforced  Polymer  Strengthened  Prestressed  Concrete   T-Beams’,Journal  of  composites  for  construction, Volume:9, Issue No:4, pp.313-326.

7) Amir  Fam  and  Trevor  Skutezky(2006), ‘Composite  T-Beams  Using  Reduced-Scale  Rectangular  FRP  Tubes  and  Concrete  Slabs’, Journal  of  Composities  for  Construction, Volume:10, Issue No:2, pp.172-181.

8) Thomas, Job,Ramaswamy, Ananth(2006), ‘Shear  Strength  of  Prestressed  Concrete  T-Beams  with  Steel  Fibers  Over  Partial/Full  Depth’, ACI  Structural  Journal , Volume:90, Issue No:1, pp.1-14.

9)  O.Alidoust,I.Sadrinejad  and  M.A.Ahmadi (2007), ‘A  Study  on  Cement  Based  Composite  Containing  Polypropylene  Fibres  and  Finely  Ground  Glass  Exposed  to  Elevated  Temperatures’, Journal  of  Science,Engineering  and  Technology, Volume:34, Issue No:2,pp.162-167.

10) M.V.KrishnaRao,N.R.Dakhshina  Murthy and V.Santhosh Kumar (2009), ‘Behaviour  of  Polypropylene  Fibre  Reinforced  Fly  Ash  Concrete  Deep  Beams  in  Flexure  and  Shear’, Journal  of  Structural  Engineering, Volume:135,Issue No:3,pp.239-252.

11) M.Z.Jumaat, M.M.Rahman  and  M.A.Alam(2010), ‘Flexural  strengthening  of  RC  continuous  T-Beam  using  CFRP  laminate’, International  Journal of  the physical Sciences, Volume:5, Issue No:6, pp.619-625.